[image: image1.png]4% =y

s
500

L Y





	GNL-5513xx  
(5x5mm RECTANGULAR TYPE)

Standard Brightness
ABSOLUTE  MAXIMUM  RATING:(Ta=25℃)
Parameter

Unit

DC Forward  Current 

30

mA

Reverse Voltage

5

V

Reverse  Current  (Vr-5V)

10

µA

Peak Forward Current ,tw ,=1 msec Duty ,=1/20

150

mA

Operation Temperature

-40

+80

℃
Storage Temperature 

-40

+100

℃
Solder  Dip

(5 seconds,1.6mm from body ) Temperature 

300

±5
℃

	[image: image2.jpg]GN‘O"R

Lighting
LED TECHNOLOGY






	Feature:                                        Description:
1.Small flange without stand-off                     1.The shape of this series is round 

2.Long life-solid state reliability                     2.General application is for indication,illumination,etc.

3.Long lead length(25.4mm)                        3.These LED lamps are available with a choice of defferent 

4.Versatile mounting on P.C. board or panel              colors,light intensities,epoxy colors,etc.



	Part Number

EMITTED COLOR

Lens Color

Peak Wavelength

(nm)

Vf

(v)

Typ.

IV (If=20mA) mcd

View Angle

2θ1/2

Min.

Typ.

GNL-5513HD

GaP

Red

Red Diffused

700

2.1

1.3

5

60°
GNL-5513GD

GaP

Green

Green Diffused

565

2.1

8

32

60°
GNL-5513YD

GaAsP

Yellow

Yellow Diffused

585
2.1

8

32

60°
GNL-5513UYD

AlGaInP
Yellow

Yellow Diffused

589
2.1

60
95
60°
GNL-5513ED

GaAsp/Gap

Orange

Red Diffused

625

2.0

8

50

60°
GNL-5513ED-E

GaAsp/Gap

Orange

Orange Diffused

635

2.0

8

50

60°
GNL-5513UED-TL
AlGaInP
Orange
Red Diffused
620
2.0
350
500
60°
GNL-5513PGD-TL
InGaN
green

Green diffused

520
2.0

450

800

60°



G-NOR ELECTRONICS CO.,LTD.








